K13 PANEL LINING SYSTEMS (IPS) Melamine faced chipboard

Supplier:  Toilet Cubicles Ireland, Unit 15 Donore business pk, donore rd, Drogheda

Co Louth, Ph/fax 0419818148

Email: info@toiletcubiclesireland.ie Web: www.toiletcubiclesireland.ie

Product reference: D1 full height duct/access panels

Panels: 19mm melamine faced made to measure panels, full height panel sets

Core material: Moisture resistant (MR) melamine faced 710kg/m3 chipboard (MFC)

Facing/Finish: Subject to MFC manufacturer selected

Colour: Toilet Cubicles Ireland MFC selection

Edge treatment: All edges lipped with matching/contrasting durable 1mm PVC

Substrate: Treated softwood framework notched, screwed made to measure and site

assembled.

Fixing of panels: Concealed Keku lift off or push fit clips/brackets

Joint treatment: Supplied with horizontal and or vertical flash gap strips in HPL

laminate

Moisture content at time of fixing: As recommended by fabricator to suit

environmental conditions as clause. Consult with Toilet Cubicles Ireland for details.

Accessories: Fixing clips, flash gap laminate strips or (19mm bonded board option

surcharge)

Dimensions: Unless stipulated dimensions/panels are as the technical data provided for

D1 duct

Other requirements: Cut outs and holes through panels marked on site by builder.

Sanitary ware schedule for panel splits and to assist in access panels being easily

removed in line with CDM guidelines